## Slide 1
TNA user feedback
Advanced microscopy characterization of
innovative ceramic coatings for hydrogen technologies
THIS PROJECT HAS RECEIVED FUNDING FROM THE EUROPEAN UNION’S HORIZON 2020 RESEARCH AND INNOVATION PROGRAMME UNDER GRANT AGREEMENT NO 823717
Elisa Zanchi
Politecnico di Torino, Italy

## Slide 2
Outline
Network and collaborations around ESTEEM3 project
The CeramECS project: “Glass-ceramic and ceramic materials for energy conversion and storage”
Motivation: Solid Oxide Cell technologies for hydrogen energy
  Ceramic protective coatings
  Electrophoretic deposition (EPD)
  Advanced TEM characterization
Further activities: the GlaMater project
Concluding remarks
Elisa Zanchi, Politecnico di Torino

## Slide 3
International Centre of Electron Microscopy for
Materials Science at the AGH-UST, Krakow, Poland
Electrophoretic deposition expertise
A.R. Boccaccini
EPD processing
F. Smeacetto, E. Zanchi
Advanced microscopy characterization
G. Cempura
Department of Applied science and Technology,
Institute of Physics, GLANCE Group, Turin, Italy
Testing & characterisation
S. Molin,
J. Ignaczak
EPD upscaling
A.G. Sabato
Industrial partner
for EU projects
Stack testing
H. Javed
Dresden, Germany
Erlangen, Germany
Barcelona,
Spain
Gdansk, Poland
GA # 700300
GA # 874577
Elisa Zanchi, Politecnico di Torino
Network and collaborations

## Slide 4
Motivation: H2 technologies
Interconnect
Solid oxide cells (SOCs) are electrochemical energy conversion
devices operating at temperatures in the range of 600–850 °C
Why SOCs?
Efficient energy conversion technology
Clean: Low GHGs emissions
Reduction of CO2 fingerprint
SOEC: Electrical energy  Chemical energy (H2)
SOFC: Chemical energy (H2) Electrical energy
rSOC: integration in renewable energy systems
30 cells stack,
Sunfire GmbH
Elisa Zanchi, Politecnico di Torino

## Slide 5
SOC stack
Grant # 874577 - NewSOC
HT corrosion
  Progressive oxidation limits the electric conductivity
  Volatile Cr-compounds degrade the cell performance
  I) Deposition of a ceramic protective coating
Gas tightness
  Need to completely avoid gas leakage
  Suppress undesired reactions
  II) Design of innovative interface concepts
Ferritic stainless-steels are widely used as interconnects SOC stacks
  Electrical connection
  Separation between oxidizing/reducing atmosphere
CeramECS
Elisa Zanchi, Politecnico di Torino
Interconnect

## Slide 6
HT corrosion
The coating must:
Reduce the oxidation rate of the steel
Reduce Cr-evaporation
Ensure high electrical conductivity
Compatible thermal expansion coefficient
(11-13 10-6 K-1)
Applying a protective coating on the steel is a promising approach to extend the interconnect life and avoid cathode poisoning
The Mn-Co spinel family (MCO) has been shown to be particularly promising
The functional properties can be improved by
Modifications with additional elements – doping
Optimized deposition and sintering
Co
Mn
Xu et al, Science 21 (2019) 19
E. Zanchi et al., J. Power Sources. 455 (2020) 227910.
Elisa Zanchi, Politecnico di Torino

## Slide 7
Electrophoretic deposition
Elisa Zanchi, Politecnico di Torino
Electrophoresis : motion of charged particles in a suspension
under the influence of an electric field
Deposition: coagulation of particles to a dense mass
m= mass deposited at time t on surface S
Cs = concentration in the suspension
µ = electrophoretic mobility
E = electric field applied
E. Zanchi, et al., Mater. Lett. 286 (2021) 129229
e = dielectric constant of the liquid.
h = viscosity of the liquid.
ζ = Zeta potential.
v = particle velocity.
Hamaker’s equation:
Experimental challenges:
Stability of the suspension
Deposition parameters
Sintering process
1) Upscale of the electrophoretic deposition set-up
2) Modification of the spinel by electrophoretic co-deposition
Compared to other techniques, EPD
Has a simple and adaptable set-up
Is a fast and versatile technique
Reduces processing time and cost
EPD set-up @ POLITO

## Slide 8
CeramECS
GA # 700300
EPD adapted to a 3-electrode set-up
̴20x20 cm surface successfully deposited
The EPD deposited
Mn–Co spinel coating showed improved stability
…to validate EPD for real dimension devices
SOC Stack test: 850 °C, 3000 h
Elisa Zanchi, Politecnico di Torino
Glass-ceramic and ceramic materials for energy conversion and storage
EPD apparatus upscale

## Slide 9
Mn-Co spinel coating
Advanced TEM post-mortem characterization
Crofer22APU
Crofer22APU
MCO EPD coating
Elisa Zanchi, Politecnico di Torino
Fib lamella:
to investigate reactions at the steel-coating interface and developed phases
Overview
of the
FIB lamella
Magnification of oxide scale-coating
interface
Crofer22APU
Oxide Scale
Oxide scale
MCO coating
Coating

## Slide 10
Overview of the FIB lamella from coated interconnect
Elisa Zanchi, Politecnico di Torino
EDS map of the lamella:
Different Mn and Co distribution in the coating
Cr confined in the oxide scale and absence of “reaction layer”
Mn-rich sub scale oxidation
Crofer22APU
Scale
Coating
Mn-Co spinel coating

## Slide 11
Elisa Zanchi, Politecnico di Torino
Experimental HAADF –STEM and Simulated HAADF STEM
Simulated SAED of Cr2MnO4, superimposed on experimental one
Mn-rich oxide scale grain
Remarkable diffusion of Mn leading to Cr-Mn spinel formation
Increased the electric conductivity and lower Cr evaporation compared to pure chromia scale
O | Cr | Mn | Fe
59.2 | 30.4 | 10.0 | 0.2
EDS composition
Oxide scale
Coating
Mn-Co spinel coating
Advanced TEM characterisation of oxide scale–coating interface

## Slide 12
Elisa Zanchi, Politecnico di Torino
At.% | O | Cr | Mn | Co | Fe
1 | 53.5 | 0.6 | 17.6 | 27.8 | 0.6
2 | 54.5 | 1.3 | 29.1 | 14.8 | 0.3
Oxide scale
Coating
1
2
Dual phase structure of the
Mn-Co spinel coating
Cobalt-rich grains: MnCo2O4 cubic structure
Mn-rich elongated grains: Mn2CoO4 tetragonal structure
Simulated SAED of Mn2CoO4 superimposed on exp.
one [ZA 301]
Advanced TEM characterisation of oxide scale–coating interface
Mn-Co spinel coating

## Slide 13
Fe-Cu co-doping of the Mn-Co spinel coating
…to improve the functional properties of the Mn-Co spinel by addition of transition metals
Two-step
Reactive sintering:
Reduction
Re-oxidation
Electrophoretic co-deposition of 3 precursors:
cathodic deposition
Successful in-situ doping: Stabilization of the cubic spinel structure
Water-ethanol suspension
Deposited on Crofer22APU
Optimised deposition at 50 V for 30 s
Four different spinel compositions
Elisa Zanchi, Politecnico di Torino
CeramECS
Glass-ceramic and ceramic materials for energy conversion and storage

## Slide 14
Doped spinel coatings
Better oxidation resistance of Fe-Cu doped coatings compared to base
Mn-Co spinel
Improved spinel stability
Synergic effect of Cu and Fe
Characterization of Mn-Co spinel coatings with Fe-Cu addition
Cu addition boosts densification
No Cr diffusion during aging
Assessment of dilatometric properties of Fe-Cu doped spinels
Elisa Zanchi, Politecnico di Torino
Fe addition
Fe+Cu addition

## Slide 15
Advanced TEM characterization of doped coatings
Fe and Cu homogeneously distributed in the coating
10Fe10Cu sample:
Highest amount of dopants
Thin oxide scale
Steel
Coating
High coating densification
Elisa Zanchi, Politecnico di Torino
Doped spinel coatings
Point c3:
Solution with CrMnCoO4
Zone axis 101
Point c2:
Solution with MnCo2O4
Zone axis 112
Point b1:
Solution with MnCo2O4
Zone axis 112

## Slide 16
5Fe5Cu sample: lowest amount of dopants
Homogeneous distribution of Fe and Cu in the Mn-Co spinel
Fe+Cu addition: synergic effect
in suppressing the double-phase spinel formation
Elisa Zanchi, Politecnico di Torino
View of the lamella from the outer coating side
Doped spinel coatings
Advanced TEM characterization of doped coatings
Point 1:
Solution with MnCo2O4
Zone axis 114
1
Steel
Coating

## Slide 17
Gas tightness
  II) Design of innovative interface concepts
Crofer22APU
.. To minimize reactions between steel and the sealant
Improve thermo-mechanical properties of the joint
GlaMater (March 2023)
HT (air)
Alumina layer
with enhanced surface roughness
Glass ceramic sealant
Crofer22APU
Alumina
Successful EPD modification:
Elisa Zanchi, Politecnico di Torino
“Advanced glass and ceramic materials for energy applications”
GlaMater
Further activities in ESTEEM3

## Slide 18
The Transnational Access
provided by ESTEEM3 Project enabled:
Elisa Zanchi, Politecnico di Torino
The consolidation of fruitful networking
Strengthening of AGH-POLITO collaboration
Publications on high-impact journals
Training on TEM characterization techniques
Professional (and personal!) experience for PhD activity
Results and publications
on the CeramECS projects provided:
A first in-depth characterization of Mn-Co dual spinel structure and oxide scale evolution after stack test at relevant conditions
A first comprehensive assessment of synergic effect of Fe-Cu addition into the Mn–Co spinel structure
Better understanding of coating degradation phenomena
  …to improve the performance and durability of SOC devices
  and boost hydrogen technologies
Krakow, 2019
Krakow, 2023
Concluding remarks

## Slide 19
Acknowledgments
This project has received funding from the Fuel Cells and Hydrogen 2 Joint Undertaking (now Clean Hydrogen Partnership) under Grant Agreement No 874577-NewSOC. This Joint Undertaking receives support from the European Union’s Horizon 2020 Research and Innovation program, Hydrogen Europe and Hydrogen Europe Research.
Thank you for the attention
elisa.zanchi@polito.it
Electrophoretic deposition, FAU, Erlangen, Germany,