## Slide 1
TNA user feedback
Nano-gold on hierarchically structured gadolinium-doped ceria as an active oxidation catalyst: synergistic effect of chemical composition and structural hierarchy
THIS PROJECT HAS RECEIVED FUNDING FROM THE EUROPEAN UNION’S HORIZON 2020 RESEARCH AND INNOVATION PROGRAMME UNDER GRANT AGREEMENT NO 823717

## Slide 2
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Motivation
Oxygen buffer
(CeIV O2 ↔ CeIV1−xCeIIIxO2−x/2)
CeO2
γ-Al2O3
Rh, Pd, Pt
Automotive catalyst
Nano-size effect
Electronic structure
Microstrain
Oxygen vaccancy concentration
Lattice parameter
EEA/Air quality in Europe – raport No 9/2020
CO
HC NOx
PM

## Slide 3
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Motivation
CeO2
γ-Al2O3
Rh, Pd, Pt
Nano-size effect
Electronic structure
Microstrain
Oxygen vaccancy concentration
Lattice parameter
Structural hierarchy
1º
2º
3º
Oxygen buffer
(CeIV O2 ↔ CeIV1−xCeIIIxO2−x/2)

## Slide 4
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Motivation
Nano-size effect
Electronic structure
Microstrain
Oxygen vaccancy concentration
Lattice parameter
doi.org/10.1016/j.jmrt.2018.12.012
Active phase deposition
Doping
REE
(rare-earth elements)
?
Structural hierarchy
1º
2º
3º

## Slide 5
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Motivation
doi.org/10.1016/j.jmrt.2018.12.012
Active phase deposition
Doping
REE
(rare-earth elements)
?
Determination of structure-activity relationship
HSMCO project goals
Description of the structural hierarchy of active catalytic supports and gold-decorated catalysts.
Determination of the Gd3+ dopant distribution throughout the system.
Determination of the distribution and location of Au NPs.
EM techniques used
HREM, EDX, EELS, HAADF-STEM, ET-HAADF

## Slide 6
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Porous rods
Nanoparticles
1°
2°
3°
CeO2
Rare-earth elements doping
Shape-selective synthesis
Porosity engineering
Ce(HCOO)3
2 µm
Synthesis
Star-shaped particles
Thermolysis
Structural hierarchy

## Slide 7
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Hierarchical structure: dopant influence
[D2]
50 %
10 %
70 %
40 %
30 %
0 %
dopant concentration
STEM-XEDS
STEM-XEDS
Global dopant distribution
Notes: Stability of particels morphology that is depenent on opant concentration
Dopant distribution: golobal and local

## Slide 8
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
[D2]
50 %
10 %
70 %
40 %
30 %
0 %
dopant concentration
DF, EELS
Microstructure
STEM-XEDS
Hierarchical structure: dopant influence
Notes: Stability of particels morphology that is depenent on opant concentration
Dopant distribution: golobal and local

## Slide 9
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
[D2]
50 %
10 %
70 %
40 %
30 %
0 %
dopant concentration
STEM-XEDS
Hierarchical structure: dopant influence
Microstructure
Raman
Notes: Stability of particels morphology that is depenent on opant concentration
Dopant distribution: golobal and local

## Slide 10
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
[D2]
50 %
10 %
70 %
40 %
30 %
0 %
dopant concentration
Raman
Hierarchical structure: dopant influence
Microstructure
dopant clustering
Notes: Stability of particels morphology that is depenent on opant concentration
Dopant distribution: golobal and local

## Slide 11
Dopant concentration
PXRD Ce1-xGdxO2-x/2
Crystal structure
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
[D2]
50 %
10 %
40 %
30 %
0 %
dopant concentration
Hierarchical structure: dopant influence
70 %
Temperature [℃]
dopant clustering
Notes: Stability of particels morphology that is depenent on opant concentration
Dopant distribution: golobal and local

## Slide 12
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Dopant concentration
Temperature [℃]
Activation energy of NPs growth
PXRD Ce1-xGdxO2-x/2
Hierarchical structure: dopant influence
Crystal structure

## Slide 13
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Dopant concentration
Temperature [℃]
PXRD Ce1-xGdxO2-x/2
NPs size
NPs strain
Rietveld refinement
Crystal structure
Hierarchical structure: dopant influence

## Slide 14
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Rietveld refinement
Evolution of the support architecture
Hierarchical structure: dopant influence
NPs size
NPs strain

## Slide 15
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Stability of the architecture in soot combustion
Hierarchical structure: dopant influence
Evolution of the support architecture

## Slide 16
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Catalytic activity
Soot combustion
Stability of the architecture in soot combustion

## Slide 17
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Active phase deposition

## Slide 18
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Filmik tomografia
Au5/ CeO2 HSNPs
Electron Tomography
Active phase deposition

## Slide 19
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Catalytic activity
CO oxidation

## Slide 20
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Synergistic effect of chemical composition and structural hierarchy
TEM data + simulation
CO chemisorption
Atom normalization
TOF
Proposed approach

## Slide 21
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Synergistic effect of chemical composition and structural hierarchy
CO chemisorption
Atom normalization
TOF
Proposed approach

## Slide 22
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Conclusions
Hydrothermal synthesis + thermolysis + deposition-precipitation -> catalyst with structural hierarchy and superior activity
Gd3+ increases activity and stability of the architecture of catalyst
Gd3+ influences the temperature-dependent evolution of the architecture
Synergistic effect of structural hierarchy and doping in propane oxidation

## Slide 23
HSMCO project
Hierarchically Structured Mixed Cerium Oxides
Thank you for your attention!
Literature
Woźniak, P., Małecka, M.A., Chinchilla, L., Trasobares, S., 3D hierarchically structured Ce1-xGdxO2-x/2 mixed oxide particles: the role of microstructure, porosity and multi-level architecture stability in soot and propane oxidation, Mater. Res. Bull., 2022, 151, 111816.
Woźniak, P., Małecka, M.A., Kraszkiewicz, P., Miśta, W., Bezkrovnyi, O., Chinchilla, L., Trasobares, S., Confinement of nano-gold in 3D hierarchically structured gadolinium- doped ceria mesocrystal: synergistic effect of chemical composition and structural hierarchy in CO and propane oxidation. Catal. Sci. Technol., 2022, 12, 7082-7113.
Woźniak P., Miśta W., Małecka M.A., Function of various levels of hierarchical organization of porous Ce0.9REE0.1O1.95 mixed oxides in catalytic activity, CrystEngComm, 2020, 22, 5914-5930.